Contact: Angela Smith

(423)553-2266

angela_smith@sind.com

SI Geosolutions’ Landlok® Turf Reinforcement Mat

with X3™ Fiber Technology Is “Fastest Way to See Green”

CHATTANOOGA, Tenn. – SI Geosolutions has developed a new fiber technology that enhances seedling emergence over traditional round or oval fibers used in conventional stitch-bonded turf reinforcement mats (TRMs).

SI’s X3™ fibers are extruded through a unique process that provides over 40 percent more surface area because of its unique shape. Landlok® TRM with X3 fiber technology is arranged in a three-dimensional pattern that creates a thick matrix of voids for trapping and housing more of the water, sediment, and seed required for rapid vegetation growth.

“Landlok with X3 fiber technology is the most advanced stitch-bonded TRM available today,” said Deron Austin, P.E., Marketing Manager for SI Geosolutions. “It is uniquely engineered for rapid seedling emergence. This means it’s the fastest way to prevent erosion, develop vegetation, and capture sediment runoff that improves storm water quality.”

TRMs are long-term, non-degradable rolled erosion control products (RECP) composed of UV stabilized synthetic fibers, nettings, or filaments processed into a three-dimensional matrix. These products are often used as a vegetative alternative to rock riprap or concrete lining systems in storm water channels.

In accordance with Erosion Control Technology Council (ECTC) Draft Test Method #4, testing showed that SI’s Landlok with X3 fiber technology facilitated a 40 percent increase over conventional stitch-bonded TRMs in seed germination and plant growth during the first 21 days. In accordance with ASTM D-6818, it exhibited 60 percent greater tensile strength, which ensures structural integrity during and after product installation. Additionally, Landlok with X3 fiber technology provided 10 percent better resiliency when tested in accordance with ASTM D-6524, which means that it provides a protective environment during the germination period when seedlings are most vulnerable.

SI Geosolutions is a world leader in providing geotextiles and erosion control products to the construction/civil engineering market, offering solutions that speed construction, improve cost-effectiveness, and raise the level of performance. SI products have also proven highly effective in American projects working to meet the EPA’s NPDES storm water regulations. For more about Landlok with X3 fiber technology, call (800)FIX-SOIL or visit www.fixsoil.com.

###